SUPPLEMENTARY MATERIALS –

Phase diagrams of the systems formed by lead fluoride with rare-earth fluorides

Pavel P. Fedorov

Eurasian Soil Science.

.

Table S1. Reference materials for calibration of thermocouples

| Substance | Melting temperature, ºC | Substance | Melting temperature, ºC |
| --- | --- | --- | --- |
| Sn | 232 | NaF | 994 |
| Pb | 327 | YF3 (phase transition) | 1070 |
| eutectic LiF+ NaF | 650 | YF3 (melting) | 1152 |
| NaCl | 800 | CaF2 | 1418 |
| LiF | 845 | LaF3 | 1500 |

Chemical Analyses.

Analyses were carried out in the Central Laboratory of the Experimental Plant at the Physical-Chemical Institute of the Academy of Sciences of the Ukrainian SSR, in Odessa. The rare-earth and lead ions were determined by complexonometric titration (Trilon B) with Xylenol Orange indicator at pH 5. The precision of analysis was ±0.5 wt %. The rare-earth ions were transferred to solution by heating fluorides with concentrated sulfuric acid on a sand bath. Lead fluoride was stripped by 40% ammonium acetate solution under gentle heating. The fluorine was determined as PbFCl precipitated upon addition of sodium chloride and lead acetate solutions in a weakly acidic medium. The excess lead was titrated trilonometrically. The stripping procedure was as follows: a 0.25-g aliquot of the sample mixed with 0.25 g of SiO2 and 6 g of Na2CO3 + K2CO3 (1:1) placed in a platinum dish was heated at 900C  for 20 min, followed by stripping with hot water. The metal carbonates remained in the precipitate; SiO2 was added to prevent the loss of fluorine. The precision of analysis was ±0.5 wt %.

Table S2. Results of the chemical analyses of the samples in the PbF2-DyF3 system after DTA.

| № | Initial content of DyF3, mol% | Conversion to evaporation of PbF2, mol% DyF3 | Results of analysis, wt.% |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Pb | Dy | F |
| 1 | 70 | 81 | Analysis data The calculation of the 80% mol % DyF3 | 18.62 18.45 | 58.57 57.87 | 23.23 23.68 |
| 2 | 35 | 49 | Analysis data The calculation of the 46% mol % DyF3 | 48.88 47.94 | 32.10 32.03 | 19.75 20.03 |
| 3 | 25 | 34 | Analysis data The calculation of the 34% mol % DyF3 | 57.82 57.83 | 23.77 23.37 | 18.77 18.80 |
| 4 | 50 | 67 | Analysis data The calculation of the 62% mol % DyF3 | 34.82 34.34 | 44.0 43.95 | 20.81 21.71 |

Table S3. DTA data for the PbF2- LaF3 system

| Composition, mol% LaF3 | T1, ºC, liquidus | T2, ºC. solidus | T3, ºC, peritectic equilibrium |
| --- | --- | --- | --- |
| 0 | 825 |  |  |
| 1 | 859 | 831 |  |
| 3.5 | 884 | 840 |  |
| 7.5 | 930 | 830 | 910 |
| 9 |  |  | 965 |
| 12.5 |  |  | 960 |
| 15 |  |  | 967 |
| 20 |  | 890 |  |
| 60 |  |  | 940 |
| 88 |  |  | 940 |
| 100 | 1500 |  |  |

Table S4. DTA data for the PbF2- CeF3 system

| Composition, mol% CeF3 | T1, ºC, liquidus | T2, ºC. solidus | T3, ºC, peritectic equilibrium |
| --- | --- | --- | --- |
| 0 | 825 |  |  |
| 1 | 870 | 840 |  |
| 2 | 874 | 840 |  |
| 3 | 890 | 840 |  |
| 6 | 925 |  |  |
| 20 |  |  | 1025 |
| 50 |  |  | 1010 |
| 87.5 |  |  | 1020 |
| 100 | 1443 |  |  |

Table 5. DTA data for the PbF2- PrF3 system

| Composition, mol% PrF3 | T1, ºC, liquidus | T2, ºC, solidus |
| --- | --- | --- |
| 0 | 825 |  |
| 1 | 859 |  |
| 3 | 900 | 840 |
| 4 | 904 |  |
| 6 | 923 | 840 |
| 7 | 944 |  |
| 12.5 | 1020 | 915 |
| 22 | 1045 |  |
| 27 |  | 976 |
| 100 | 1404 |  |

Table 6. DTA data for the PbF2- NdF3 system

| Composition, mol% NdF3 | T1, ºC, liquidus | T2, ºC, solidus |
| --- | --- | --- |
| 0 | 825 |  |
| 2 | 859 |  |
| 2.5 | 869 | 828 |
| 5 | 888 | 840 |
| 6.5 | 900 |  |
| 8 | 935 |  |
| 10 | 957 | 864 |
| 18 |  | 900 |
| 100 | 1372 |  |

Table 7. DTA data for the PbF2- SmF3 system

| Composition, mol% SmF3 | T1, ºC, liquidus | T2, ºC, solidus | T3, ºC, peritectic equilibrium |
| --- | --- | --- | --- |
| 0 | 825 |  |  |
| 2 | 876 | 840 |  |
| 5 | 919 | 860 |  |
| 9 | 970 |  |  |
| 13 | 1029 |  |  |
| 15 | 1018 | 930 |  |
| 23 |  | 990 |  |
| 37.5 |  |  | 1080 |
| 80 |  |  | 1080 |
| 100 | 1304 | 470* |  |

- - transformation

Table 8. DTA data for the PbF2- GdF3 system

| Composition, mol% GdF3 | T1, ºC, liquidus | T2, ºC | T3, ºC |  |
| --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |
| 2 | 855 | 831 |  |  |
| 5 | 895 | 847 |  |  |
| 6 | 900 |  |  |  |
| 10 | 945 | 880 |  |  |
| 11 | 955 |  |  |  |
| 18 | 987 | 930 |  |  |
| 20 |  | 931 |  |  |
| 23 | 1005 |  |  |  |
| 27 | 1013 | 970 |  |  |
| 35 | 1020 |  |  |  |
| 43 | 1032 |  | 783 |  |
| 51 | 1030 |  | 782 |  |
| 57.5 | 1027 |  |  |  |
| 61 | 1032 |  | 785 |  |
| 80 | 1030 |  |  |  |
| 100 | 1230 |  |  | 1070 |

Table 9. DTA data for the PbF2- TbF3 system

| Composition, mol% TbF3 | T1, ºC, liquidus | T2, ºC | T3, ºC | T4, ºC | T5, ºC |
| --- | --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |  |
| 6 | 900 | 841 |  |  |  |
| 11 | 936 |  |  |  |  |
| 13 | 943 |  |  |  |  |
| 19 | 970 | 932 |  |  |  |
| 26 | 985 |  |  |  |  |
| 33 | 996 |  |  |  |  |
| 35 | 995 |  |  |  |  |
| 38 | 998 |  |  |  |  |
| 39 | 998 |  | 820 |  |  |
| 42 | 997 | 985* | 823 |  |  |
| 43 | 991 | 991 | 820 |  |  |
| 44 |  | 983 |  |  |  |
| 47 |  | 984 |  |  |  |
| 48 |  | 985 | 816 |  |  |
| 49 |  | 989 | 818 |  |  |
| 50 | 1028 | 985 | 820 |  |  |
| 53 |  | 992 | 815 |  |  |
| 55 | 1047 | 990 |  |  |  |
| 58 |  | 992 | 817 |  |  |
| 60 | 1085 | 993 | 819 |  |  |
| 64 |  | 985 | 820 |  |  |
| 67 |  | 987 | 816 |  |  |
| 70 |  | 991 |  |  |  |
| 75 | 1120 | 985 |  |  |  |
| 78 |  | 981 |  | 810 |  |
| 93 |  |  |  |  | 1120 |
| 100 | 1166 |  |  |  |  |

Table 10. DTA data for the PbF2- DyF3 system

| Composition, mol% DyF3 | T1, ºC, liquidus | T2, ºC | T3, ºC | T4, ºC | T5, ºC |
| --- | --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |  |
| 3 | 880 | 833 |  |  |  |
| 6.5 | 888 | 838 |  |  |  |
| 10 | 918 | 840 |  |  |  |
| 13 | 945 |  |  |  |  |
| 17 | 964 |  |  |  |  |
| 18 |  | 932 |  |  |  |
| 22 | 968 | 950 |  |  |  |
| 25.5 | 966 |  |  |  |  |
| 27 | 969 |  |  |  |  |
| 29.5 | 972 |  |  |  |  |
| 33 | 968 |  |  |  |  |
| 36 |  | 967 |  |  |  |
| 39 | 972 |  |  |  |  |
| 42 |  | 948 | 830 |  |  |
| 45 | 957 |  |  |  |  |
| 46 | 962 | 953 |  |  |  |
| 47 |  | 953 | 847 |  |  |
| 50 | 966 | 942 | 840 |  |  |
| 51 |  | 953 | 840 |  |  |
| 54 | 977 | 957 | 825 | 908 |  |
| 56 | 985 | 957 | 830 |  |  |
| 60 |  | 946 | 840 |  |  |
| 62 | 1018 | 942 | 820 | 880 |  |
| 69 | 1060 | 965 |  | 903 |  |
| 76 | 1075 | 967 |  | 891 |  |
| 77 |  | 967 |  | 901 | 1069 |
| 79 |  | 961 |  |  |  |
| 81 |  | 969 | 825 | 891 | 1055 |
| 85 | 1128 | 966 |  | 900 | 1056 |
| 91 |  | 960 |  |  | 1043 |
| 100 | 1147 |  |  |  |  |

Table 11. DTA data for the PbF2- HoF3 system

| Composition, mol% HoF3 | T1, ºC, liquidus | T2, ºC | T3, ºC | T4, ºC | T5, ºC |
| --- | --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |  |
| 5 | 884 | 839 |  |  |  |
| 10 |  | 874 |  |  |  |
| 12 | 915 | 886 |  |  |  |
| 19 | 942 | 914 |  |  |  |
| 23 | 960 | 934 |  |  |  |
| 27.5 | 960 | 956 |  |  |  |
| 32 | 959 | 945 |  |  |  |
| 36 | 951 | 944 |  |  |  |
| 38 | 954 |  |  |  |  |
| 42 |  | 922* | 852 |  |  |
| 43 | 943 | 923* | 865 |  |  |
| 48 | 930 | 925 | 862 |  |  |
| 50 | 923 | 923 | 861 |  |  |
| 56 |  | 925 | 862 |  |  |
| 58 | 967 | 925 | 870 |  |  |
| 63 |  | 935 | 865 | 973 | 895 |
| 64 |  | 935 | 865 | 978 | 895 |
| 70 | 1020 |  |  | 976 | 896 |
| 72 |  |  |  | 972 |  |
| 80 |  |  | 853 | 975 |  |
| 100 | 1140 |  |  |  |  |

Table 12. DTA data for the PbF2- ErF3 system

| Composition, mol% ErF3 | T1, ºC, liquidus | T2, ºC | T3, ºC | T4, ºC |
| --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |
| 5.5 | 882 | 836 |  |  |
| 10 | 916 |  |  |  |
| 12 | 920 | 870 |  |  |
| 17 | 929 | 895 |  |  |
| 19 | 931 |  |  |  |
| 22 | 940 | 927 |  |  |
| 24 | 940 |  |  |  |
| 28 | 947 | 942 |  |  |
| 30 | 948 |  |  |  |
| 32 |  | 937 |  |  |
| 35 | 941 | 920 | 842 |  |
| 38 | 934 |  | 865 |  |
| 43 | 922 | 882 |  |  |
| 46 | 908 | 886 | 863 |  |
| 52 |  | 900 | 852 |  |
| 55 |  | 906 |  |  |
| 63 |  | 900 | 865 |  |
| 73 |  | 900 | 866 |  |
| 76 |  | 900 |  |  |
| 78 | 1050 | 900 | 862 |  |
| 87 |  | 898 | 866 |  |
| 88 |  | 898 | 870 |  |
| 96 |  | 900 | 868 | 1000 |
| 100 | 1134 |  |  | 1104 |

Table 13. DTA data for the PbF2-TmF3  system

| Composition, mol% TmF3 | T1, ºC, liquidus | T2, ºC | T3, ºC | T4, ºC |
| --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |
| 6 | 870 | 843 |  |  |
| 17 | 918 | 897 |  |  |
| 19 | 918 |  |  |  |
| 26 | 916 | 900 |  |  |
| 31 | 908 |  |  |  |
| 37 | 901 | 880 | 860 |  |
| 38 | 893 | 880 |  |  |
| 45 |  | 880 | 860 |  |
| 47 |  | 880 | 860 |  |
| 56 |  |  | 856 |  |
| 66 |  | 870 | 856 |  |
| 74 | 976 |  | 860 |  |
| 78 | 1000 |  | 862 |  |
| 100 | 1159 |  |  | 1047 |

Table 14. DTA data for the PbF2-YbF3  system

| Composition, mol% YbF3 | T1, ºC, liquidus | T2, ºC | T3, ºC | T4, ºC |
| --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |
| 6 | 860 | 853 |  |  |
| 10 | 893 | 865 |  |  |
| 12 | 900 | 882 |  |  |
| 15 |  | 888 |  |  |
| 17 | 907 | 900 |  |  |
| 19 | 905 | 905 |  |  |
| 23 | 907 | 904 |  |  |
| 26 | 904 |  |  |  |
| 28 | 904 |  |  |  |
| 33 | 888 | 850* |  |  |
| 36 | 877 | 850* |  |  |
| 37 | 887 | 850* |  |  |
| 39 | 870 | 850* |  |  |
| 41 | 865 | 850* |  |  |
| 43 | 867 | 850* |  |  |
| 46 | 853 | 850* |  |  |
| 49 |  |  | 843** |  |
| 53 |  |  | 841** |  |
| 54 |  |  | 847** |  |
| 56 |  |  | 843** |  |
| 61 |  |  | 835** |  |
| 63 |  |  | 843** |  |
| 66 |  |  | 843** |  |
| 69 |  |  | 841** |  |
| 72 |  |  | 842** |  |
| 75 |  |  | 839** |  |
| 80 |  |  | 980 | 840** |
| 100 | 1155 |  | 978 |  |

* - peritectic equilibrium

** - eutectic equilibrium

Table 15. DTA data for the PbF2-LuF3  system

| Composition, mol% LuF3 | T1, ºC, liquidus | T2, ºC | T3, ºC | T4, ºC |
| --- | --- | --- | --- | --- |
| 0 | 825 |  |  |  |
| 5 | 856 | 841 |  |  |
| 10 | 880 | 845 |  |  |
| 11.5 | 880 | 865 |  |  |
| 12.5 | 880 | 865 |  |  |
| 14 | 888 |  |  |  |
| 17 | 880 | 878 |  |  |
| 19 | 878 |  |  |  |
| 30 | 873 |  | 826 |  |
| 33 | 871 |  | 830 |  |
| 35 | 856 |  | 826 |  |
| 37.5 | 854 |  | 820 |  |
| 40 |  |  | 817 |  |
| 44 |  | 802 | 822 |  |
| 48 | 812 | 796 |  |  |
| 51 |  | 796 |  |  |
| 55 |  | 793 |  |  |
| 59 |  | 796 |  |  |
| 66 |  | 800 |  |  |
| 73 |  | 797 | 931 |  |
| 75 |  | 799 | 934 |  |
| 80 |  | 793 | 910 |  |
| 83 |  | 792 | 928 |  |
| 85 | 1060 | 802 | 929 |  |
| 100 | 1152 |  | 953 |  |